## Slide 1
AI autonomous operation proposal · Landscape
Landscape: precedent research
Subsystem
Who they are & what exactly they demonstrated
Source
RHEED online analysis
PNNL — Pacific Northwest National Laboratory (US DOE; Kaspar et al.). Built RHAAPsody, an unsupervised, material-agnostic on-the-fly RHEED analyzer: pretrained-CNN features + changepoint detection + graph clustering over the pattern sequence. On live TiO2 MBE growth the full workflow ran in <1 s/frame and flagged transitions ~1 min faster than the human expert. Open source. Perception only — active control is their stated next phase.
JVST A 43, 032702 (2025)
GitHub: pnnl/RHAAPSODY
MBE real-time closed loop
Chinese Academy of Sciences (Shen et al.) and follow-up QD-laser work. Trained a 3D ResNet-50 on RHEED video (not stills) to predict InAs/GaAs quantum-dot density during growth, then closed the loop on the MBE: density dialed anywhere across 3.8×10⁸–1.4×10¹¹ cm⁻² (~2.5 orders of magnitude), fully automated. The 2025 follow-up self-optimized QD-laser growth in-run: PL 3.2× the manually-optimized baseline, FWHM 36.7→28.2 meV, ~0.85 s per decision.
Nat. Commun. 15, 2724 (2024)
QD-laser (2025, PMC)
MBE unattended operation
IVWorks — Korean GaN epiwafer foundry. DOMM Agent: deep-learning RHEED embedding + an agent driving the MBE control PC; scheduled runs execute load–grow–unload unattended on nights/holidays with real-time pass/fail prediction. Commercial existence proof of the whole route — but no yield / unattended-hours / dispersion figures have been published; cite strictly as a vendor claim.
IVWorks announcement (Jun 2025)
Autonomous experimentation (real sputter tool)
Empa — Swiss Federal Laboratories for Materials Science and Technology (Wieczorek, Siol et al.). Ran autonomous Bayesian sampling (BayBE / BoTorch GP) on a real bipolar-HiPIMS magnetron sputter rig: >3,000 process conditions across a 6-D pulse-parameter space collected unattended, SHAP-interpreted, data released CC-BY. Their scientific finding was itself negative (positive pulse mostly reduces deposition rate) — we cite the autonomous method and dataset; our RIG kernel passed its calibration acceptance on exactly this dataset.
Digital Discovery (2026)
Zenodo dataset (CC-BY-4.0)
Self-driving PVD to a target spec
npj Computational Materials (2025) — self-driving sputter lab. Fully autonomous silver-film deposition: sputter hardware + in-situ optical spectroscopy + Bayesian ML with no human in the loop, aborting unpromising runs early. Hit the target optical spec in 2.3 attempts on average (vs 3.6 for the ablated baseline), 98 s per measurement cycle, >20,000 data points over 38 samples.
npj Comput. Mater. (2025)
Run-to-run APC + virtual metrology
Industry practice (PVD). Published sputter-APC case: EWMA run-to-run control compensating target-erosion drift lifted Cpk from <1.4 to >2.0 — a retrospective simulation on historical fab data (vendor case study, not an audited production number). Tree-ensemble virtual metrology for PVD film properties: Chen et al., ISA Transactions 103 (2020).
Spotfire sputter-APC article
Notes: Sourcing caveats — state these if challenged on any figure: • IVWorks DOMM: vendor marketing only. No published yield, unattended-hours or dispersion numbers. Cite as existence proof of the commercial route, never as a numeric benchmark. DOMM is not sold externally. • Empa (Digital Discovery 2026): the paper's own scientific conclusion is negative — positive pulsing is broadly unfavourable for deposition rate. We cite the autonomous methodology and the real dataset, not any claim that autonomy improves rate. • Sputter APC Cpk <1.4 → >2.0 is a vendor case study in retrospective simulation, not an audited result. • The commonly cited estimate that APC is worth >US$300M/yr to a 20K wafer/month logic fab is a consultancy figure, not independently audited. Quote it only with that qualification. • RHAAPsody is a perception benchmark. It does not perform active control; our pipeline extends its methodology.

## Slide 2
AI autonomous operation proposal · Problem definition
Problem definition
Process quality on MBE and PVD still rests on the operator's judgement in the moment. RHEED patterns are read by eye; target erosion and chamber drift on PVD are compensated through periodic spot checks and engineering experience. Three manufacturing problems follow.
01
Latency
A human reacts to an anomaly in minutes. Growth-stage transitions — AlN nucleation giving way to streak recovery — open and close in seconds.
02
Not reproducible
The same recipe spreads across shifts and operators. That spread is one of the main sources of yield loss.
03
Does not scale
Doubling capacity means doubling skilled engineers, and skilled engineers cannot be produced on that schedule.
Objective
Run the equipment unattended: judge process state from in-situ signals, correct the control variables, and turn engineering intuition into an auditable, reusable software asset.
What "autonomous agent" means here — the strict definition
Sense
→
State estimate
(with uncertainty)
→
Decide
→
Independent check
→
Bounded action
→
Full audit trail
Every link carries an acceptance gate. When an input falls outside the model's competence, the system must return INFEASIBLE with a diagnosis rather than force an answer.
→
Learn & refit
Data flywheel — part of the loop, not a separate system: every audited run returns as training data, so more data → sharper models → better decisions across the whole system. The agent improves itself by operating.
Notes: Three manufacturing problems, the strict definition of autonomy used in this proposal, and the data flywheel that compounds across runs.

## Slide 3
AI autonomous operation proposal · Target workflow
Target intelligent autonomous workflow
Data model
Learn / calibrate + optimize
MBE / PVD (equipment)
Control + monitoring system
Measurement feedback
Local LLM orchestrator
Reason + instruct
Run to run
In-situ
Ex-situ
optimize
Input
Output wafer
Output data
feedback
control
control
Notes: Target loop: the data model proposes a recipe, the equipment runs it under in-situ RHEED sensing, measurement feedback returns to the model; the local LLM reasons over the run and issues control.

## Slide 4
AI autonomous operation proposal · Existing foundation
Existing foundation: in-house software
01
Data model
Recipe-Inverse Generator (RIG)
A forward model from recipe to result, plus an inverse solver that back-calculates candidate recipes. The aim is to find recipes that meet the requirement.
Verified
Tested on Empa's real magnetron sputtering HiPIMS (PVD) dataset
Next
Validation on real tool data
02
Sensing and control
RHEED Analysis
A CNN + ViT computer vision pipeline for image analysis and monitoring. The aim is to find transition points and use an LLM to interpret them and act.
Verified
Tested on two sets of real TiO2 RHEED data
Next
GaN RHEED validation + tool validation
03
Physical simulation
MBE Simulation
A simulation model of the MBE chamber built from physics.
Verified
Underlying physics built out and refined
Next
Calibration against real tool data
Notes: Current status and next step for the three in-house assets; none has yet been validated on this project's own tool.

## Slide 5
AI autonomous operation proposal · 07 Autonomy roadmap
Autonomy ladder and engineering specification
Level
Scope
Entry conditions (qualitative for now — numeric gates set after baseline measurement)
L1
Observe
Read-only acquisition; full data capture during runs
Data contract accepted: every signal captured and logged with trustworthy time synchronisation; the ingest validation layer proven by fault injection to actually reject bad data.
L2
Shadow
AI issues decisions with rationale; nothing is written to the tool
Model calibration passes its acceptance check on our own tool data; perception agrees with expert judgement consistently across a sustained shadow period.
L3
Supervised loop
Single variable, then multivariable (MBE, PVD); one-click engineer takeover at every step
Control law clears the full fault-injection suite in simulation; write-back latency verified against fast-loop needs; watchdogs and clamps proven in red-then-green drills; every recipe change passes the independent confirmation gate before it touches the tool.
L4
Unattended
Continuous unattended operation
Supervised operation stable over a sustained period; EHS and insurance sign-off in writing; unattended and fallback drills (network loss, heartbeat loss, sensor failure) all passed.